## Slide 1: Epistemic and Aleatory Uncertainty Quantification of Fatigue Crack Growth Analysis
John McFarland and Erin DeCarlo
October 23, 2019

## Slide 2: Outline and objectives
Influence of limited data for determining input distributions
Methods for separating and combining epistemic/aleatory uncertainty in probabilistic analysis
  Enhancements to NESSUS® software
Demonstration using probabilistic fatigue crack growth analysis

## Slide 3: Background and motivation
Two related efforts focused on development of methods and tools for quantification of multiple uncertainty types
2.5-year program with AFRL and turbine engine consortium
  Epistemic and aleatory uncertainty quantification for turbine engine lifing applications
4-year DARPA Open Manufacturing program
  Framework for rapid qualification of new materials and manufacturing processes

## Slide 4: Probabilistic analysis with multiple uncertainty types
Uncertainties:
Aleatory (scatter)
Epistemic (knowledge)
Deterministic model (e.g., life prediction)
Model
Performance
Model Inputs
Probabilistic modeling of inputs to separate aleatory and epistemic uncertainty
Double-loop sampling to propagate inputs through deterministic model
Variance-based sensitivity analysis to identify key drivers for reducible uncertainty
Approach
Bounds due to epistemic uncertainty
Predicted life, with quantified uncertainty and sensitivity
Example variables shown for illustration
Example finite element model
Epistemic
Aleatory
Design life
Life
Material Properties

## Slide 5: Small fatigue crack growth: Problem definition
Published experimental data
  Ti-6Al-2Sn-4Zr-6Mo
  Round-bar geometry with micro-notch
Uncertain variables
  Equivalent crack initiation depth
    Based on 16 experimental measurements
  Crack growth rate parameters (C, n)
    Based on reported C, n values from 7 fatigue tests
Crack growth analysis set up using NASGRO® software
NASGRO K solution for surface crack (SC07)
S. Jha, R. John, and J. Larsen. Incorporating small fatigue crack growth in probabilistic life prediction: Effect of stress ratio in Ti-6Al-2Sn-4Zr-6Mo. International Journal of Fatigue 51, pp. 83-95, 2013.
(a)
Jha et al. (2013)
Jha et al. (2013)
Example crack initiation site
Notes: Small crack behavior of interest because it drives life-limiting behavior and exhibits increased specimen-to-specimen variability

## Slide 6: Demonstration goals
Objectives:
  Quantify aleatory and epistemic uncertainty in:
    Initial flaw size
    Crack growth rate parameters (C, n)
  Compute probabilistic response for crack growth life (risk) with quantified confidence
  Quantify relative effects of limited data for flaw size and crack growth rate
Questions:
  Should more data be collected for initial flaw size?
  Should more data be collected for crack growth rate?
NASGRO K solution for surface crack (SC07)
(a)
Jha et al. (2013)
Jha et al. (2013)
Example crack initiation site

## Slide 7: Step 1: Define uncertainty models for inputs
Epistemic and aleatory uncertainty is defined for two inputs to the analysis
  Initial crack size (aeq) based on 16 data points
  Crack growth rate model parameters (C, n) based on values from 7 repeat tests
Epistemic uncertainty quantified using Bayesian inference
  Select form of probability distribution for aleatory uncertainty
  Determine posterior distribution for parameters:
: Distribution parameters
: Data
Posterior
Prior
Likelihood

## Slide 8: Probabilistic model for initial crack size
Modeled aleatory and epistemic uncertainty based on 16 data points
Used lognormal probability distribution
  Epistemic uncertainty in mean and std. dev. based on available data
CDF of aeq with Bounds due to Epistemic Uncertainty
Epistemic Uncertainty on aeq
Distribution Parameters
Lognormal paper

## Slide 9: Crack growth rate data
Power-law model used to describe crack growth rate in terms of C and n parameters
Modeled aleatory and epistemic uncertainty in joint distribution for (C,n) based on 7 data points
Used bivariate normal distribution and included uncertainty in correlation coefficient
Power-law representations for results from 7 crack growth tests
Observed scatter in crack growth rate model parameters

## Slide 10: Uncertainty model for crack growth rate
Bayesian inference captured uncertainty in 5 distribution parameters based on observed data
Statistical model included:
Specimen-to-specimen variability
Epistemic uncertainty
Aleatory:
Epistemic:
Model fit using Markov Chain Monte Carlo sampling

## Slide 11: Step 2: Create response surface model
Fast-running RSM enables large number of calculations needed for nested Monte Carlo and variance decomposition
Steps for RSM creation:
  Identify variables (aeq, C, n)
  Define variable bounds for DOE
  Generate DOE points and run performance model to collect training data
    NESSUS automates this process (in our case, running NASGRO)
  Fit RSM and assess goodness of fit
    NESSUS and/or NESSUS Response Surface Toolkit

## Slide 12: Response surface model
Used NESSUS to interface with NASGRO and perform a DOE with 100 cases
Fit resulting training data to a Gaussian Process model using NESSUS Response Surface Toolkit
RSM predicts cycles to failure based on 3 variables: aeq, C, and n
2-dimensional RSM slice for aeq= 5μm
Leave-one-out cross-validation

## Slide 13: Step 3: Uncertainty propagation and sensitivity analysis
NESSUS is used to propagate the uncertainties in the 3 random variables through the response surface model
Predict CDF of crack growth life, with uncertainty bounds
Sensitivity analysis conducted in two ways:
  Sensitivity of probabilistic results (CDF) to epistemic uncertainties (i.e. where to collect more data)
  Relative sensitivity of performance (crack growth life) to aleatory and epistemic components of uncertainty

## Slide 14: Computed probability distribution for crack growth life, with uncertainty bounds
Inherent variability in initial crack size and crack growth rate propagated through analysis
Confidence bounds show effect of epistemic uncertainty due to limited data
Lognormal probability paper
Sample sizes:
million

## Slide 15: Sensitivity to epistemic uncertainties
NESSUS can isolate the effect of the epistemic uncertainties with respect to any probability point on the CDF
Here, sensitivities computed with respect to the “minus 2 sigma” value of crack growth life
What new data should be collected to reduce uncertainty?
Crack growth rate properties
Crack size

## Slide 16: Sensitivity to epistemic uncertainties
Epistemic uncertainty in the crack growth rate parameters is the main driver. Additional data on initial crack size would have negligible impact.
Crack growth rate properties
Crack size
J. McFarland, Variance decomposition for statistical quantities of interest, Journal of Aerospace Information Systems 12 (1) (2015) 204-218.
What new data should be collected to reduce uncertainty?

## Slide 17: Uncertainty reduction scenario study (1)
Demonstration of effect of hypothetical new data for CG rate
Validate conclusions from sensitivity analysis that primary source of uncertainty is CG rate
(a)
(c)
(b)
(d)

## Slide 18: Uncertainty reduction scenario study (2)
Demonstration of effect of hypothetical new data for crack size
Validate conclusions from sensitivity analysis that epistemic uncertainty in crack size not important
(a)
(c)
(b)
(d)

## Slide 19: “Predictive” distribution shows combined influence of both uncertainty types
NESSUS can compute a single CDF called the “Predictive distribution”
This CDF reflects the effect of both aleatory and epistemic uncertainties in the crack growth life predictions
Combined effect of aleatory and epistemic uncertainty
Requires only “single-loop” Monte Carlo:

## Slide 20: Relative sensitivities of both uncertainty types
NESSUS can also analyze relative contributions of both uncertainty types in predictive distribution
In this example, inherent variability in crack growth rate is primary driver
But, epistemic uncertainty is also contributing
Epistemic
Aleatory
S. Sankararaman, S. Mahadevan, Separating the contributions of variability and parameter uncertainty in probability distributions, Reliability Engineering & System Safety 112 (2013) 187-199.

## Slide 21: Summary
Initial crack size
Probability distribution parameter uncertainty
Contact: john.mcfarland@swri.org
Novel variance decomposition to separate uncertainty types
Integrated computational tools
Probabilistic results with quantified uncertainty

## Slide 22
Appendix

## Slide 23: Monte Carlo simulation
MC simulation propagates aleatory uncertainty in model input variables
j = 1 to N
Performance function
Aleatory:
But this assumes that we know the statistical properties of the input variables (epistemic uncertainty is ignored)…

## Slide 24: Double-loop uncertainty propagation
Epistemic:
Nested Monte Carlo approach quantifies confidence in predictions by separating the effects of aleatory and epistemic uncertainty
Uncertainty in performance for given probability
Uncertainty in probability for given performance
j = 1 to N_inner
i = 1 to N_outer
Aleatory:
Performance function

## Slide 25: Mixed-loop uncertainty propagation
“Predictive” distribution
i = 1 to N
Epistemic:
Aleatory:
Performance function
“Auxiliary variable” approach allows evaluation of relative contributions of aleatory and epistemic uncertainty
“Mixed-loop” approach combines both uncertainty types into a single probabilistic prediction
Epistemic
Aleatory
(a)
(a)

## Slide 26: Sensitivity analysis for uncertainty reduction
(a)
(b)
Goal: Identify what new data are needed in order to most efficiently reduce epistemic uncertainty
Example: Have 100 data points for initial flaw size and 20 data points for material properties. What additional data should be collected?
Approach: Novel application of variance decomposition to isolate epistemic uncertainties in probabilistic predictions
J.M. McFarland. "Variance Decomposition for Statistical Quantities of Interest", Journal of Aerospace Information Systems, Vol. 12, Special Section on Uncertainty Quantification (2015), pp. 204-218.

## Slide 27: Crack growth rate UQ
Statistical model included:
Specimen-to-specimen variability
Epistemic uncertainty
Aleatory:
Epistemic:
Monte Carlo samples and density contours for posterior predictive distribution (aleatory + epistemic uncertainty)