## Slide 1: Hybrid Probabilistic Model for Resistance of Pressure Tube Material in Canadian Nuclear Reactors to Crack Initiation due to Hydrided Region Overloads
Fourth International Symposium on
Probabilistic Methodologies for Nuclear Applications
Leonid Gutkin and Doug Scarth
Kinectrics Inc.
Toronto, Ontario, Canada
Leicester, UK
November 1 - 3, 2022

## Slide 2: Introduction
Distinction is often made between:
  Analytical probabilistic models – based primarily on concepts and theories
  Empirical probabilistic models – based primarily on experimental information
Such distinction is often not well-defined in engineering applications
  Hybrid probabilistic models with both analytical and empirical sub-models
  In particular, hybrid probabilistic models of material performance and degradation are quite common
Different sources of uncertainty are involved in analytical models and in empirical models
Development of hybrid probabilistic models
is associated with unique challenges

## Slide 3: Outline
Background
Analytical Framework
Empirical Sub-Models
Hybrid Probabilistic Model
Summary

## Slide 4: Background
Pressure tubes in CANDU ® reactors
® CANDU is a registered trademark of Atomic Energy of Canada Ltd.
CANDU reactor core: 380 to 480 fuel channels
with nuclear fuel and pressurized heavy water coolant

## Slide 5: Background
Hydride-assisted cracking in CANDU pressure tubes
Formation and growth of Zr hydrides at in-service flaws
Zr-2.5Nb pressure tubes
Corrosion reaction of Zr-based material with heavy water (D2O)
Increasing content of hydrogen, in the form of deuterium (D)
Preferential diffusion of hydrogen to locations of stress concentration
In-service flaws in Zr-2.5Nb pressure tubes are evaluated for hydride-assisted cracking
Potential fracture of hydrides under applied loads
Potential crack initiation:
(a) under sustained operation
(b) during pressure transients

## Slide 6: Background
Hydrided region overload events
Time
Normal operation
Temperature
Pressure
Low-power hot state
Cool-down and heat-up
hydrided region overload event: applied stress exceeds hydride formation stress
Low-power hot state
Normal operation
terminal hydrogen solubility: dissolution
terminal hydrogen solubility: precipitation
hydride formation
non-ratchetting
ratchetting

## Slide 7: Background
Crack initiation criteria
peak flaw-tip stress at hydride formation
overload resistance
critical peak flaw-tip stress for crack initiation due to hydrided region overloads during pressure transients
threshold peak flaw-tip stress for initiation of delayed hydride cracking (DHC) under constant pressure during sustained operation
Delayed hydride cracking under constant pressure
Hydrided region overloads during pressure transients

## Slide 8: Background
Observed trends in overload resistance
Generally, overload resistance tends to increase:
  As temperature increases
  As resistance to DHC initiation increases
For given hydride formation conditions, overload resistance tends to increase as flaw geometry becomes less severe:
  Larger flaw root radius
  Smaller flaw depth
  Smaller ratio of flaw length to flaw depth
For given flaw geometry, overload resistance tends to increase:
  As applied stress during hydride formation decreases
  When applied stress is reduced prior to hydride formation (reactor de-pressurization)
  Under non-ratchetting hydride formation conditions (hydrides are completely dissolved under sustained reactor operation)

## Slide 9: Analytical Framework
Threshold stress for DHC initiation
Physics-based, analytical process-zone model is used to predict
threshold stress for initiation of delayed hydride cracking (DHC) under
sustained reactor operation and ratchetting hydride formation conditions
threshold stress intensity factor for DHC initiation from crack-like flaw
threshold stress for DHC initiation at planar surfaces
yield stress
flaw depth
tube wall thickness
flaw root radius
From: “Technical Requirements for In-service Evaluation of Zirconium Alloy Pressure Tubes in CANDU Reactors”, Canadian Nuclear Standard CSA N285.8:21, CSA Group, 2021.
flaw geometry
material properties

## Slide 10: Analytical Framework
Dual process-zone approach
Two flaw-tip displacements in a hydrided region *
vhf : displacement due to hydride formation
vml : displacement due to plastic deformation of Zr-2.5Nb matrix ligaments
* Dual process-zone approach originally developed by Professor E. Smith
threshold stress for DHC initiation under sustained operation (constant applied loads)
applied stress during hydride formation

## Slide 11: Analytical Framework
Baseline model formulation
overload crack initiation exponent
overload crack initiation coefficient

## Slide 12: Analytical Framework
Overload crack initiation exponent
lower rate of change
higher rate of change

## Slide 13: Empirical Sub-Models
Scope and hierarchy
Empirical sub-models to adapt dual process-zone approach to broad range of flaw geometries, hydride formation conditions and evaluation temperatures
Currently, mechanistic understanding is not sufficient to develop an entirely analytical model for overload resistance
Overload resistance at arbitrary temperature
Effects of flaw geometry
Overload resistance at low reference temperature
Effect of evaluation temperature
Effects of hydride formation conditions

## Slide 14: Empirical Sub-Models
Hydride non-ratchetting factor for DHC initiation
hydride non-ratchetting factor for DHC initiation
threshold stress for DHC initiation under ratchetting hydride formation conditions *
[NR] = 0: ratchetting
[NR] = 1: non-ratchetting
* Analytical process-zone model (Slide 9)
equivalent hydrogen concentration
rate-of-change parameter
shape parameter

## Slide 15: Empirical Sub-Models
Overload crack initiation exponent
hydride formation factor
rate-of-change parameter
rate-of-change parameter
number of non-ratchetting thermal cycles since flaw formation
[NR] = 0: ratchetting
[NR] = 1: non-ratchetting

## Slide 16: Empirical Sub-Models
Overload crack initiation coefficient
hydride formation factor
rate-of-change parameter
index of stress reduction prior to hydride formation
flaw geometry factor
flaw depth
flaw length
rate-of-change parameter
shape parameter
stress concentration factor
offset parameter
flaw root radius
temperature factor

## Slide 17: Empirical Sub-Models
Temperature factor for overload resistance
QhfT represents effect of hydride formation conditions and DHC initiation resistance on temperature factor
high reference temperature
power-law coefficient
BTΘ , BTZ and TZ0 are parameters for temperature factor
TL is low reference temperature (= room temperature)

## Slide 18: Hybrid Probabilistic Model
Model structure
effects
sub-models
Hybrid model
Analytical sub-model
Empirical sub-model
Overload resistance
(ratio of critical stress for overload crack initiation to hydride formation stress)
Overload crack initiation coefficient
Overload crack initiation exponent
Resistance to
DHC initiation
Effects of material properties
Effects of hydride formation conditions
Effects of flaw geometry
Effect of temperature

## Slide 19: Hybrid Probabilistic Model
Multi-variable nonlinear regression -
Overload resistance at room temperature
Four model parameters are characterized simultaneously
residual error
best-estimate prediction

## Slide 20: Hybrid Probabilistic Model
Multi-variable nonlinear regression -
Temperature factor for overload resistance
residual error
best-estimate prediction
Two model parameters are characterized simultaneously

## Slide 21: Hybrid Probabilistic Model
Example predictions: room temperature

## Slide 22: Hybrid Probabilistic Model
Example predictions: room temperature

## Slide 23: Hybrid Probabilistic Model
Example predictions: temperature trends

## Slide 24: Hybrid Probabilistic Model
Example predictions: temperature trends

## Slide 25: Summary
Hybrid probabilistic model has been developed for resistance of CANDU Zr-2.5Nb pressure tubes to crack initiation due to hydrided region overloads
Analytical modelling framework
  Adaptation of dual process-zone methodology originally developed by Professor E. Smith
  Overload resistance is power-law function of resistance to DHC initiation under constant applied stress
  Coefficient and exponent vary with flaw geometry and hydride formation conditions
Overload resistance increases with evaluation temperature
  Temperature factor varies with flaw geometry and with hydride formation conditions
  Variations are qualitatively consistent with those for overload resistance at room temperature

## Slide 26: Summary
Analytical sub-model for resistance to DHC initiation
  Effect of evaluation temperature
  Effects of flaw geometry
  Effects of hydride formation conditions
  Effects of material properties
Empirical sub-model for overload crack initiation coefficient
  Effect of evaluation temperature
  Effects of flaw geometry
  Effects of hydride formation conditions
Empirical sub-model for overload crack initiation exponent
  Effects of flaw geometry
  Effects of hydride formation conditions
Model is suitable for use in both deterministic and probabilistic fitness-for-service evaluations of CANDU Zr-2.5Nb pressure tubes

## Slide 27: Acknowledgements
Professor E. Smith developed dual process-zone approach that forms the theoretical basis for this work
G.K. Shek of Kinectrics Inc. contributed to development of model formulation
Valuable discussions held with:
  D. Cho and M. Ip of Bruce Power LP
  G. Bickel and H. Chaput of Canadian Nuclear Laboratories
  M. Baghbanan, J. Lam and P. Le-Dreff Kerwin of Ontario Power Generation Inc.
  J. Cui, P. Doddihal, T. Hunt, C. Liu, C. Manu, D.H.B. Mok,
  P. Mosbrucker and S.X. Xu of Kinectrics Inc.
Experimental data provided by CANDU Owners Group
Funding provided by CANDU Owners Group

## Slide 28: Concluding Remarks
William H. Press
    “Simulation and mathematical modeling will power the 21st century the way steam powered the 19th.”
George E.P. Box
    “Remember that all models are wrong; the practical question is how wrong do they have to be to not be useful.”