## Slide 1: PROBABILISTIC LEAK-BEFORE-BREAK EVALUATION OF SMALL LINE DISSIMILAR METAL WELDS USING xLPR
4th International Symposium on Probabilistic Methodologies for Nuclear Applications
November 1-3, 2022, Leicester, UK
Nov 1, 2022
C. Harrington, N. Glunt, D.J. Shim
Electric Power Research Institute
N. Cofie, M. Uddin
Structural Integrity Associates, Inc.

## Slide 2: Outline
Background
Objectives
Probabilistic Input and Approach
Case Studies
Summary

## Slide 3: Background
To meet GDC-4 requirements, deterministic LBB (SRP 3.6.3) has been applied
  SRP 3.6.3 requires that all degradation mechanisms be evaluated to demonstrate they are not potential sources of pipe rupture
  Prior to early 2000, only fatigue crack growth was considered for LBB evaluations to address normal operating transient cycles
  SRP 3.6.3 requires margins of 10 on leakage and 2 on critical through-wall crack length
PWSCC in PWR DM welds found early 2000 – an active degradation mechanism
  PWSCC morphology reduces the LBB margins
  MRP-140 – LBB margins were maintained for large diameter piping (>12 inch)

## Slide 4: Background (cont’d)
xLPR developed by NRC/EPRI - a PFM software tool to demonstrate the low probability of rupture requirement in GDC-4
  Developed under rigorous software QA program
  Reports from NRC Office of Regulatory Research - demonstrated extremely low probability of rupture for large diameter piping
Application of LBB to small diameter piping (<6 inch) is challenging
  Requires very low leak detection capabilities to meet SRP 3.6.3 margins
  Previous study shows LRD of 0.1-0.5 gpm is required for NPS 4 to NPS 6

## Slide 5: Objective
Probabilistic evaluation using xLPR for a small diameter piping nozzle with a dissimilar metal (DM) butt weld susceptible to PWSCC
  Feasibility study to determine if xLPR can be used to demonstrate LBB acceptance for small diameter piping from a probabilistic viewpoint
Sensitivity studies include
  Two different weld residual stress (WRS) profiles
  Flaw coalescence (multiple and long surface flaws)
  The effect of mitigation by weld overlay (WOL)

## Slide 6: Probabilistic Input Parameters (xLPR)
Pipe Dimensions: Representative Spray Nozzle
  OD: 143.3 mm (5.64 in)
  Thickness: 23.9 mm (0.94 in) (Ri/t = 2.0)
Materials: Alloy 82/182, SA-508 CS, 316 SS
  Properties from xLPR v2.1 materials library
Loads: Plant specific CE pressurizer spray nozzle
  15.5 MPa and 320.5⁰ C
Weld residual stress (WRS): discussed on Slide 7
Realizations: 400-800K
Initial flaw distribution: lognormal distribution
  Depth: 1.5 mm median with 1.419 ln()
  Length: 4.8mm median with 2.226 ln()
PWSCC Growth Rate: MRP-115
Inspection Scenarios: one inspection every 10 years
POD curves: obtained from xLPR User Manual
Leak rate detection (LRD): discussed on Slide 8
Load | Type | Stress, MPa (ksi)
Internal Pressure | Membrane | 23.27 (3.38)
Crack Face Pressure* | Membrane | 15.51 (2.25)
Deadweight | Membrane | -0.35 (-0.05)
 | Bending | 1.47 (0.21)
Thermal Expansion | Membrane | -0.14 (-0.2)
 | Bending | 7.55 (1.1)
SSE | Membrane | 0.30 (0.04)
 | Bending | 35.99 (5.22)

## Slide 7: WRS Distributions Applied
Unmitigated WRS
Two unmitigated WRS distributions are used in this study
  MRP-106 WRS for 5-in safety relief nozzle (25% OD weld repair)
  CE-plant spray nozzle WRS (50% pre-service repair)
The CE plant-specific WRS has higher tensile stresses at the inside surface of the pipe
Mitigated WRS
Two mitigated WRS distributions are used in this study
  WOL WRS 1 – stress-free, 50% preservice repair, WOL
  WOL WRS 2 – original DMW, 50% preservice repair, WOL
Stress mitigation technique - Weld Overlay (WOL)
Both WRS profiles show compressive residual stress on the inner half of the DM butt weld

## Slide 8: Leak Rate Detection (LRD)
Typical LRD in deterministic LBB (SRP 3.6.3) – 1.0 gpm
Lower LRD is required to meet the required LBB margin for small diameter piping
  Previous study based on fatigue crack morphology shows LRD of 0.1-0.5 gpm is required for NPS 4 to NPS 6
Several plants were able to justify a leak detection limit of 0.25 gpm
NRC Reg. Guide 1.45, Rev 1 stated that with improvements in leakage monitoring system and data analysis, plants can detect leakage lower than 0.05 gpm
In this study, an LRD range of 0.1-10 gpm is investigated

## Slide 9: Deterministic LBB Evaluation: SRP 3.6.3
For the subject small diameter DM butt weld, a leak detection capability of 0.07 gpm is required to meet the SRP 3.6.3 margin

## Slide 10: Probabilistic Approach using xLPR
Probability of failure of a postulated through-wall crack – analogous to the SRP 3.6.3 approach.
However, realistic case would be to start with a surface crack
  Scenario 1
    Start with a surface crack
    Grow it to a through-wall flaw (all surface cracks may not grow to through-wall cracks)
    Grow the though-wall flaw to LRD or rupture
  Scenario 2
    Start with a surface crack
    Grow it to full circumferential crack
    Rupture without LRD
Pf is the probability of failure
Psc is the probability of surface crack rupture
PTWC is the probability of a through-wall leaking crack
Pf|TWC is the conditional probability of failure given a through-wall crack
xLPR direct output

## Slide 11: Case Studies
Single surface flaw
  Effect of WRS profiles
  Effect of mitigations
Multiple and long circumferential surface cracks (180⁰ - 270⁰)
  Effect of WRS profiles
  Effect of mitigations

## Slide 12: Acceptance Criteria for Probabilistic LBB
The Acceptance Group of the xLPR project recommended acceptance criteria for a probabilistic analysis is less than 1E-06 failures per year
This acceptance criteria was also used in recently published two reports from the NRC Office of Regulatory Research
  The same acceptance criteria is used in the current work

## Slide 13: Single Flaw Case: Two WRS Profiles
LRD (gpm) | Cum. Prob. of Leak, PTWC | Cum. Prob. of Rupture, Pf | Cum. Prob. of Surface Crack Rupture, Psc | Cum. Cond. Prob. of Rupture, Pf¦TWC
MRP-106 WRS distribution |  |  |  | 
0.1 | 0.631 | 3.33E-04 (266) | 3.33E-04 (266) | N/A
1 | 0.631 | 3.33E-04 (266) | 3.33E-04 (266) | N/A
5 | 0.631 | 3.51E-04 (281) | 3.51E-04 (281) | N/A
10 | 0.631 | 3.74E-04 (299) | 3.51E-04 (281) | 3.65E-05 (18)
CE spray nozzle WRS distribution |  |  |  | 
0.1 | 0.999 | 1.25E-06 (1) | 1.25E-06 (1) | N/A
1 | 0.999 | 1.25E-06 (1) | 1.25E-06 (1) | N/A
5 | 0.999 | 1.25E-06 (1) | 1.25E-06 (1) | N/A
10 | 0.999 | 8.37E-05 (67) | 1.25E-06 (1) | 8.25E-05 (66)
MRP-106 WRS – PTWC relatively low with relatively high PSC
  These cases not captured by deterministic LBB and LRD doesn’t play a significant role due to high Psc
CE Spray Nozzle WRS – PTWC close to 1 which implies PSC is very low
  Pf is dependent on LRD due to higher through-wall crack ruptures
For LRD 1-5 gpm, all leaks are readily detectable leading to no through-wall crack ruptures
For LRD 10 gpm, timely leak detection is not assured for all leaking cracks leading to some through-wall crack ruptures
* Numbers in the parenthesis indicate number of failure from 800K simulations
800,000 realizations

## Slide 14: Single Flaw Case: Two WRS Profiles (cont’d)
LRD (gpm) | Cum. Prob. of Leak, PTWC | Prob. of Rupture per Year | Cond. Prob. of Rupture per Year, Pf¦TWC
MRP-106 WRS distribution |  |  | 
0.1 | 0.631 | 4.16E-06 (3) | N/A
1 | 0.631 | 4.16E-06 (3) | N/A
5 | 0.631 | 4.39E-06 (4) | N/A
10 | 0.631 | 4.68E-06 (4) | 4.56E-07
CE spray nozzle WRS distribution |  |  | 
0.1 | 0.999 | 1.56E-08 (0) | N/A
1 | 0.999 | 1.56E-08 (0) | N/A
5 | 0.999 | 1.56E-08 (0) | N/A
10 | 0.999 | 1.05E-06 (1) | 1.03E-06 (1)
Per yearly basis and LRD 1-5 gpm
  Pf for MRP-106 WRS is slightly higher than acceptance criteria (4E-06 vs. 1E-06)
  Pf for CE spray nozzle WRS is two orders below the acceptance criteria (1.5E-08 vs. 1E-06)
WRS profiles play an important role for small pipe diameter nozzle
Since Pf close to acceptance criteria, the low probability of rupture could potentially be demonstrated for the small piping nozzle DM welds
* Numbers in the parenthesis indicate number of failure from 800K simulations

## Slide 15: Insight on Surface Crack Ruptures
K values are lower for MRP-106 case
  Lower leak probabilities (0.631 vs 0.999)
Higher Pf for MRP-106 WRS case mainly due to surface crack ruptures
  Kdeep goes negative – slowing/arresting crack toward depth dir.
  Ksurface stays positive – growing around circumference
Lower Pf for CE spray nozzle WRS case – mostly through-wall cracks at 10 gpm LRD
  Both Kdeep and Ksurface always stay positive
Through-wall crack ruptures tend to only occur when the LRD is high
  Leaks are allowed to grow (10 gpm) before detection
Due to surface crack ruptures, the deterministic concept of LBB should be cautiously applied to small diameter piping nozzles with DM Welds Susceptible to PWSCC

## Slide 16: Single Flaw with Mitigations
For all LRD cases (1-10 gpm) with 800K realizations
  No ruptures occurred when WOL mitigation was applied
Mitigated WRS

## Slide 17: Long Circumferential Surface Cracks
Case | Prob. of Leak, PTWC | Prob. of Rupture per Year w/ LRD | Prob. of Rupture per Year w/ LRD & ISI | Prob. of Surface Crack Rupture per Year w/ LRD
Unmitigated WRS |  |  |  | 
MRP-106 WRS (180°) | 0.91 | 1.09 E-05 (4) | 5.19E-07 (~0) | 1.09E-05 (4)
CE Spray Noz WRS (180°) | 1 | 0 | 0 | 0
Mitigated WRS |  |  |  | 
WOL WRS-1 (180°) | 0 | 0 | 0 | 0
WOL WRS-2 (180°) | 2.5E-06 | 0 | 0 | 0
WOL WRS-2 (270°) | 0 | 3.13E-08 (~0) | 2.53E-15 (~0) | 3.13E-08 (~0)
Unmitigated WRS – 180⁰ flaw
  MRP-106 WRS case - Failures were by surface crack ruptures
  CE spray nozzle WRS case - No failure in 400K realizations
Mitigated WRS
  180⁰ - No failures in 400K realizations
  270⁰ - Pf is two orders below the acceptance criteria – all surface crack ruptures
    Pf is essentially zero (2E-15) with ISI (LRD has no effect on surface crack ruptures)
LRD – 0.1 gpm
400,000 realizations

## Slide 18: Summary
As per the deterministic LBB evaluation (SRP 3.6.3), an LRD of 0.07 gpm is required to meet the SRP 3.6.3 margin whereas probabilistic evaluations using xLPR, a low probability of rupture (<1E-06) can be demonstrated with an LRD as high as 10 gpm.
  SRP 3.6.3 is very conservative for small diameter nozzle DM welds
The WRS distribution influences the probability of rupture
  One case shows Pf close to acceptance criteria
  The other case shows Pf well below acceptance criteria
For small diameter piping with unmitigated WRS distributions, failures were mainly by surface crack ruptures – against the assumption of through-wall flaw in deterministic LBB
When mitigated by WOL, the probability of rupture is essentially zero for an initial small surface flaw
For 270⁰ long circumferential surface crack,
  Mitigated, low LRD and ISI
  The probability of rupture is well below the acceptance criteria
More studies are required for general conclusion
  Additional small diameter piping nozzles and associated WRS distributions

## Slide 19: Backup Slides

## Slide 20: Material Properties
Material Property | Probabilistic Parameters |  |  |  |  |  | 
 | Distribution | Alloy 82/182 (Weld) |  | SA-508 CS (Left Pipe) |  | 316 SS (Right Pipe) | 
 |  | Mean | Std. Dev. | Mean | Std. Dev. | Mean | Std. Dev.
Yield Strength, MPa (ksi) | Lognormal | 316.5 (45.9) | 55.0 (8.0) | 399 (57.9) | 68 (9.9) | 197.1 (28.6) | 54 (7.8)
Ultimate Strength, MPa (ksi) | Lognormal | 542.0 (78.6) | 26.8 (3.9) | 629 (91.2) | 38 (5.5) | 440.4 (63.9) | 67 (9.7)
Elastic Modulus, MPa (ksi) | Normal | 196,800 (28,542) | 29,520 (4,281) | 174,960 (25,376) | 26244 (3,806) | 176,660 (25,622) | 26,490 (3,842)

## Slide 21: Long circumferential surface cracks
Case | Cumulative Prob. of Leak, PTWC | Cumulative Prob. of Rupture w/ LRD, Pf¦LRD | Cumulative Prob. of Rupture w/ LRD & ISI, Pf¦LRD-ISI | Cumulative Probability of Surface Crack Rupture w/ LRD, Psc | Probability of Rupture per Year w/ LRD | Probability of Rupture per Year w/ LRD & ISI | Probability of Surface Crack Rupture per Year w/ LRD
Unmitigated WRS |  |  |  |  |  |  | 
MRP-106 WRS (180°) | 0.91 | 8.75E-04 | 4.15E-05 | 8.75E-04 | 1.09 E-05 | 5.19E-07 | 1.09E-05
CE Spray Noz WRS (180°) | 1 | 0 | 0 | 0 | 0 | 0 | 0
Mitigated WRS |  |  |  |  |  |  | 
WOL WRS-1 (180°) | 0 | 0 | 0 | 0 | 0 | 0 | 0
WOL WRS-2 (180°) | 2.5E-06 | 0 | 0 | 0 | 0 | 0 | 0
WOL WRS-2 (270°) | 0 | 2.50E-06 | 2.02E-13 | 2.50E-06 | 3.13E-08 | 2.53E-15 | 3.13E-08

## Slide 22: Single Flaw Case: Two WRS Profiles
LRD (gpm) | Cumulative Prob. of Leak, PTWC | Cumulative Probability of Leak after 80 Years. PTWC | Cumulative Prob. of Rupture, Pf | Cumulative Probability of Rupture after 80 Years, Pf | Cumulative Prob. of Surface Crack Rupture, Psc | Cumulative Probability of Surface Crack Rupture after 80 Years, Psc | Cumulative Conditional Probability of Rupture, Pf¦TWC | Probability of Rupture per Year, Pf | Conditional Probability of Rupture per Year
MRP-106 WRS distribution |  |  |  |  |  |  |  |  | 
0.1 |  | 0.631 |  | 3.33E-04 (266) |  | 3.33E-04 (266) | N/A | 4.16E-06 (3) | N/A
1 |  | 0.631 |  | 3.33E-04 (266) |  | 3.33E-04 (266) | N/A | 4.16E-06 (3) | N/A
5 |  | 0.631 |  | 3.51E-04 (281) |  | 3.51E-04 (281) | N/A | 4.39E-06 (4) | N/A
10 |  | 0.631 |  | 3.74E-04 (299) |  | 3.51E-04 (281) | 3.65E-05 (18) | 4.68E-06 (4) | 4.56E-07
CE spray nozzle WRS distribution |  |  |  |  |  |  |  |  | 
0.1 |  | 0.999 |  | 1.25E-06 (1) |  | 1.25E-06 (1) | N/A | 1.56E-08 (0) | N/A
1 |  | 0.999 |  | 1.25E-06 (1) |  | 1.25E-06 (1) | N/A | 1.56E-08 (0) | N/A
5 |  | 0.999 |  | 1.25E-06 (1) |  | 1.25E-06 (1) | N/A | 1.56E-08 (0) | N/A
10 |  | 0.999 |  | 8.37E-05 (67) |  | 1.25E-06 (1) | 8.25E-05 (66) | 1.05E-06 (1) | 1.03E-06 (1)
* Numbers in the parenthesis indicate number of failure from 800K simulations